## Slide 1
SEM ANALYSIS
In this image we can identify the Surface of the AM part, particularly the size of the bead, some superficial imperfections as well as the interbead gaps. The size of the bead is around 400 micrometers, while the gap could reach dimensions of 50 micrometers. We observe in red some resin poor regions being of size 50 micrometers in their longest dimensión on average. The Purple zones identify resin rich regions, wich are larger in extension than resin poor regions. In Blue we can see some interbead gaps defects, possibly scarps.
SAMPLE INFORMATION: The following images correspond to sample 1 , which was an AM composite manufacture from carbon fiber and Nylon White, with reinforcement in 90°. Sample was evaluated in pure tension.

## Slide 2
In this images we can identify the slip planes of 90° samples it is to note the relatively flat surface generated as well as the serrated profile. The crack path sequencing can be deduced the fiber region fails first then the surface.

## Slide 10
SAMPLE INFORMATION: The following images correspond to sample2, which was an AM composite manufacture from carbon fiber and Nylon White, with a Layer configuration as indicated. Sample was evaluated in pure compression originating a buckling.

## Slide 24
SAMPLE INFORMATION: The following images correspond to sample3, which was an AM composite manufacture from carbon fiber and Nylon White, with a Layer configuration as indicated 0°. Sample was evaluated in pure tension originating brittle fracture